Advantages of the simple summation method described in the previous sheets

- First and Foremost, it was a very simple effort to reproduce the demagnetization factor values, which were obtained and tabulated in very early works on magnetic materials. Those Calculations which could yield such Tables of demagnetization factor values were rather complicated and required setting up elliptic integrals which had to be evaluated.

- Secondly, the principle involved is simply the convenient point dipole approximation of the magnetic dipole. And, the method requires hypothetically dividing the sample to be consisting of closely spaced spheres and the radii of these magnetized spheres are made to hold a convenient fixed ratio with their respective distances from the specified site at which point the induced fields are calculated. This fixed ratio is chosen such that for all the spheres the point dipole approximation would be valid while calculating the magnetic dipole field distribution.

- The demagnetization factors have been tabulated only for such shapes and shape factors for which the magnetization of the sample in the external magnetic field is uniform when the magnetic susceptibility of the material is the same homogeneously through out the sample. This restricts the tabulation to only to the shapes, which are ellipsoids of rotation. Where as, if the magnetization is not homogeneous through out the sample, then, there were no such methods possible for getting the induced field values at a point or the field distribution pattern over the entire specimen. The present method provides a greatly simplified approach to obtain such distributions.

- It seems it is also a simple matter, because of the present method, to calculate the contributions at a given site only from a part of the sample and account for this portion as an independent part from the remaining part without having to physically cause any such demarcations. This also makes it possible to calculate the field contribution from one part of the sample, which is within itself a part with homogeneously, magnetized part and the remaining part being another homogeneously magnetized part with different magnetization values. Hence a single specimen which is inherently in two distinguishable part can each be considered independently and their independent contribution can be added.

For the point 1 mentioned above view the web page URL:

http://saravamudhan.tripod.com/